A Proposal for Listing S31603 and S31608 in GTR

1. Background

As described in GTR, in all applications where steel comes in contact with hydrogen, hydrogen compatibility should be demonstrated. The following steels AISI316L, SUS316L, DIN1.4435 and AISI316 are recognized as suitable for high pressure hydrogen gas applications in B6.2.1.6 Metal hydrogen compatibility in the GTR.

2. Proposal

The steels S31603 and S31608 in GB 24511-2009 Stainless Steel Plate, Sheet and Strip for Pressure Equipment have similar chemical composition, mechanical properties, which are shown in Table A and Table B, as the austenitic stainless steels listed in GTR. S31603 and S31608 have been successfully used in high pressure hydrogen storage vessels with maximum pressure 77MPa. We propose to list steels S31603 and S31608 in GTR.

Table A  Chemical composition compared

| Steel | Chemical composition /% |
| --- | --- |
|  | C | Mn | Si | Cr | Ni | P | S | Mo |
| AISI316L | 0.03 | 2.00 | 0.75 | 16.0～18.0 | 10.0～14.0 | 0.045 | 0.03 | 2.00～3.00 |
| SUS316L | 0.03 | 2.00 | 1.00 | 16.0～18.0 | 12.0～15.0 | ≤0.045 | ≤0.03 | 2.00～3.00 |
| DIN1.4435 | 0.03 | 2.00 | 1.00 | 16.5～18.5 | 12.5～15.0 | ≤0.045 | ≤0.03 | 2.50～3.00 |
| S31603 (022Cr17Ni12Mo2) | 0.03 | 2.00 | 0.75 | 16.0～18.0 | 10.0～14.0 | 0.035 | 0.020 | 2.00～3.00 |
| AISI316 | 0.08 | 2.00 | 0.75 | 16.0～18.0 | 10.0～14.0 | 0.045 | 0.03 | 2.00～3.00 |
| S31608 (06Cr17Ni12Mo2) | 0.08 | 2.00 | 0.75 | 16.0～18.0 | 10.0～14.0 | 0.035 | 0.020 | 2.00～3.00 |

Table B  Mechanical properties compared (ambient temperature)

| Steel | Product forms1 | Product conditions | Rm/MPa | Rp0.2/MPa | Percentage elongation after fracture/% | Hardness |
| --- | --- | --- | --- | --- | --- | --- |
| AISI316L | B | Hot working and annealed | 480 | 170 | 40 | — |
|  | B | Cold working 2 and annealed | 480 | 170 | 30 | — |
|  | W | Annealed | 480 | 170 | — | — |
| SUS316L | — | Solution treatment3 | 481 | 176 | ≥40 | ≤90HRB；≤187HB |
| DIN1.4435 | — | Quenching | 450~700 | 195 | ≥45 | 120~180HB |
| S31603 (022Cr17Ni12Mo2) | — | Solution treatment 4 | 490 | 180 | 40 | ≤95HRB；≤217HRB |
| AISI316 | B | Hot working and annealed | 515 | 205 | 40 | — |
|  | B | Cold working 2 and annealed | 515 | 205 | 30 | — |
|  | W | Annealed | 515 | 205 | — | — |
|  | P, Sh, St | Annealed | 515 | 205 | 40 | ≤95HR |
| S31608 (06Cr17Ni12Mo2) | — | Solution treatment 4 | 520 | 205 | 40 | ≤95HRB；≤217HRB |

Note: 1. B—bar, W—wire, P—panel, Sh—sheet, St—strip.

2. the thickness＞13mm.

3. 1010~1150℃sharp quenching.

4. 1010~1150℃rapid cooling.